The microbial ecology of moderately thermophilic mineral leaching reactors: The effect of solids loading and organic carbon supplementation on reactor performance

Jonathan Dean, Robert P van Hille and Susan T.L. Harrison

Centre for Bioprocess Engineering Research, Department of Chemical Engineering, University of Cape Town, South Africa.  Sue.Harrison@uct.ac.za

Keywords: Mineral bio-oxidation, microbial ecology, solids loading, organic carbon

Abstract: Tank bioleaching of refractory sulphidic gold ores is well established, with potential to expand application to base metal concentrates. With increasing commercial tank bioleaching operations, understanding their microbial consortia is essential for process robustness. Recently, it has been shown that the consortia implicated in tank mineral bioleaching of gold-containing pyritic ores are dynamic, responding to the leaching environment. Factors driving the microbial dynamics of these consortia are under investigation, with emphasis also placed on determining the metabolic role of the key players in these consortia.

Here, the combined influence of solids loading and organic carbon availability on microbial community dynamics and performance has been studied in agitated, aerated slurry bioreactors at 45C. The control (autotrophic) and experimental (organic carbon added) reactors performed comparably at low solids loadings (4%, 7% and 10%). At 20% solids loadings, higher ferric iron concentrations (31 g/L vs 25g/L) and sulphide oxidation (66% vs 45%) were observed in the experimental reactor over the control. Under operating conditions used, a shift from bacterially-dominated cultures with L.ferriphilum as major species towards increasing archaeal abundance was observed.  Archaeal abundance was higher in the organic carbon supplemented reactor at all solids loadings. The increased microbial diversity with organic supplementation appears to contribute to increased community robustness and associated leaching with increasing stress.

Introduction:

Tank bioleaching of refractory sulphidic gold ores has become an established mining technology over the past 25 years [1]. With the existence of an increasing number of commercial tank bioleaching operations, the understanding of the microbial consortium active in these systems is essential to optimising process robustness [2, 3]. Recently, substantial deviation in the consortium composition from the expected main role players has been observed [1, 4], these being the autotrophic iron oxidising Leptospirillum ferriphilum, mixotrophic sulphur oxidising Acidithiobacillus caldus and iron/sulphur oxidising At. ferrooxidans, found in large scale operations [3]. Heterotrophic archaea such as Acidiplasma cupricumulans and Thermoplasma spp., previously less abundant have been reported to be increasingly prevalent in large scale tanks [1, 2, 4]. The bioleaching microbial community responds to physical forces in the reactor such as mixing, solids loading, particle size, aeration and chemical forces such as heavy metals, organic carbon, acidity and nutrients; these may affect culture evolution [1, 3-6]. Increased solids loading in agitated, aerated bioreactors has been shown to affect iron oxidation negatively.  The archaea have been recognised to be more vulnerable to higher solids loading than bacteria [5-7].

Several studies have shown that a variety of organic acids may be released or “leaked” into the bulk liquid from autotrophic bacteria such as A.caldus and L.ferriphilum [2, 8, 9]. These organics are a by-product of the metabolic activity of these iron or sulphur oxiders and may sustain populations of heterotrophic archaea such as the Acidiplasma and Thermoplasma spp. [9]. Communities including heterotrophs have been shown to be more effective in terms of bioleaching efficiency because dissolved organic carbon is removed [8, 9], providing a mutualistic relationship between these micro-organisms.  In this paper, we investigate the effect of organic carbon availability on the microbial ecology and the reactor performance of tank biooxidation with increasing solids loading.

Materials and Methods:

Mineral concentrate and microbial culture: All reactor experiments were conducted with the pyrite/arsenopyrite (35-75µm) concentrate provided by Fairview mine, Barberton, South Africa. The microbial consortium was created from a mixture of Fairview and Kazakstan BIOX commercial cultures maintained on Fairview arsenopyrite.

Experimental system:  Each 1 Litre glass reactor (height 0.18 m; internal diameter 0.10 m), with four equi-spaced vertical baffles, was agitated by a 4 bladed pitch blade impeller (diameter 0.057 m) operated at 400 rpm. The reactors were sparged with air at 1 vvm using an L-shaped sparger. The reactor studies were initiated with 200 ml adapted commercial culture, 40g arsenopyrite concentrate and 800 ml 0K media (pH 1.3) and maintained at 45C using a circulating heated water bath. A 20 ml slurry sample was removed from each reactor daily and analysed for redox potential (Ag/AgCl reference electrode), pH , ferrous and ferric iron (1-10 phenanthroline method, [10]). Every 24 h, 150 ml slurry was replaced with 150 ml of 0K media and the appropriate amount of Fairview concentrate to maintain the solids loading. The experimental reactor was supplemented daily with yeast extract to maintain a concentration of 0.02% (w/v) yeast extract. At each solids loading, genomic DNA was extracted for quantitative PCR analysis with two domain and 5 species specific primers [1, 11]. Cell counts were performed with the use of a Thoma counting chamber. LECO analysis was also performed to determine the extent of sulphide oxidation.

Results and Discussion

The performance of the reactors in the presence and absence of organic carbon supplementation and with increasing solids loading is given in terms of pH and redox profiles (Figure 1) and ferrous and ferric iron concentrations (Figure 2).  The control (autotrophic) and experimental (supplemented with organic carbon) reactors maintained a high redox potential (>680 mV) at the lower solids loadings (4, 7 and 10%), indicating efficient iron oxidation. At 20% solids loading, the control reactor redox decreased to ~550 mV. The redox of the experimental reactor decreased to~610 mV, before recovering to above 680 mV.

The iron, pH data and ferrous/ferric iron data indicated that performance of the control and experimental reactors was similar at low solids loadings.  On increased loading to 20%, iron oxidation performance was negatively impacted with the increasing presence of residual Fe2+.  This was more marked in the control reactor. The ferric iron concentration in solution was higher in the experimental reactor at 20% solids loadings (31 g/L) than the control reactor (25 g/L) (Fig 2). Similarly, sulphur oxidation (leading to reduced pH) was reduced in the control reactor.

7%

4%

10%

15%

20%

Figure 1: Redox potential and pH values determined for the control and experimental bioleaching reactors at each solids loading.

20%

15%

10%

7%

4%

Figure 2: Ferrous and ferric iron concentrations with the Control and Experimental reactors at each solids loading.

Table 1 : Extent of sulphide oxidation in leached arsenopyrite concentrate from control and experimental reactors

| Solids Loading (%) | Control (%) | Experimental (%) |
| --- | --- | --- |
| 4 | 81.6 | 80.2 |
| 7 | 81.5 | 81.5 |
| 10 | 67.0 | 69.2 |
| 15 | 41.9 | 57.5 |
| 20 | 45.0 | 66.0 |

Figure 3: Cell concentration ( control,  expt) and COD ( control,  expt) at each solids loading.

Cell concentrations within the control reactor were lower than the experiment, particularly at high solids loadings (Figure 3), indicating a possible increase in heterotrophic archaea with increased organic carbon concentrations [8, 9] at higher solids, measured by chemical oxygen demand (COD). The microbial diversity of the cultures is given in Figure 4.  This qPCR analysis relates major microbial classes previously identified in bioleaching of sulphide minerals [1, 11]. L.ferriphilum was dominant in both cultures at solids loadings below 20%.  The presence of Archaea was more dominant in the experimental reactor than the control, as expected from their heterotrophic nature [2]. The dominance of the Archaea increased with solids loading as previously reported by van Hille et al. [1].  This was especially notable in the experimental reactor.  Gplasma, a heterotrophic Thermoplamsa spp., was identified in both reactors; its role is not currently known [12].  The sulphide oxidation achieved (Table 1) was comparable at the lower solids loadings (4, 7 and 10%). At 20% solids loading, the experimental reactor attained 66% sulphide oxidation, compared with 45% in the control.  This performance is lower than that reported under similar operating conditions but differing reactor configuration in our labs [1]; this will be investigated further.

Figure 4: Microbial ecology with solids loading: Control (C); Experimental (E) reactors.

Conclusions

Solids loading and organic carbon supplementation influenced the tank bioleaching community evolution. At low solids concentrations, the cultures were dominated by the bacteria At. caldus and L.ferriphilum with the latter dominating.  The Archaeal abundance was higher in the reactor supplemented with organic carbon. At 20% solids, L.ferriphilum abundance was much reduced, with increased archaeal abundance, especially A.cupricumulans. This shift in bioleaching community was more marked in the carbon-supplemented reactor. The performance of the carbon-supplemented reactor at 20% solids loading exceeded the control reactor, possibly owing to the enhanced microbial diversity. Synergistic interactions between autotrophic and heterotrophic micro-organisms have been confirmed in supporting experiments (data not shown).

References

[1] 	Van Hille, R.,van Wyk, N, Froneman,T.,Harrison, S.T.L: Adv. Mater. Res. (2013), Vol.  825, p331-334.

[2]	Okibe,N.,Johnson,D.B.: Biotechnol. Bioeng. (2004), Vol. 87, p(574-583.

[3] 	Rawlings, D., Johnson, B.: Biomining . (Springer, 2007).

[4] 	van Hille R.P, van Wyk N. and Harrison S.T.L: In Biohydrometallurgy: Biotech key to unlock mineral resources value. Proceedings of 19th International Biohydrometallurgy Symposium.

[5]	Nemati,M., Harrison, S.T.L: J. Chem. Technol. Biotechnol. (2000), Vol. 75, p526-532.

[6] 	Deveci H.: Hydrometallurgy (2004), Vol. 71, p385-396.

[7] 	Harrison STL, Sissing A, Raja S, Pearce SJA, Lamaignere V and Nemati M: In Proceedings of the 15th International Biohydrometallurgy Symposium (2003).  p359-375.

[8]	Aston,J.E., Apel,W.A.,Lee,B.D.,Peyton,B.M: World J. Microbiol. (2011), Vol. 27(1), p153-161

[9] 	Ñancucheo,I., Johnson,D.B.: Appl. Environ. Microbiol. (2010), Vol. 76(2), p461-467

[10]	Komadel P. and Stucki J.W.: Clays and Clay Minerals (1998), Vol. 36(4), 379-381.

[11] Tupikina O.V, Minnaar S.H., van Hille R.P., van Wyk N., Rautenbach G.F., Dew D. and Harrison S.T.L.: Miner. Eng. (2013), Vol. 53, p152-159

[12] Justice N.B, Pan C., Mueller R, Spaulding S.E., Shah V., Sun C.L., Yelton A.P., Miller C.S., Thomas B.C., Shah M., VerBerkmoes N., Hettich R. and Banfield J.F.: Appl. Environ. Microbiol. (2012), Vol. 78(23), p8321-8330.