Enhancing ARD Mitigation by Application of Benign Tailings to Reduce the Permeability of Waste Rock Dumps

Athanasios Kotsiopoulos and Susan T. L. Harrison*

Centre for Bioprocess Engineering Research (CeBER), Department of Chemical Engineering, University of Cape Town, Rondebosch 7701, South Africa

*correspondence: Sue.Harrison@uct.ac.za, +27-(0)21-650-5501

Keywords: Acid Rock Drainage, permeability, benign tailings, waste rock dumps

Abstract. ARD mitigation is considered by reducing the permeability of acid-generating coal interburden waste rock dumps. Fine desulfurised benign tailings were used to conceal exposed surface active sites from air, water and more aggressive sulfur- and iron-oxidizing microorganisms in acidic environments. Test columns containing interburden waste rock co-disposed with benign tailings were configured as either alternating layered covers or as a blended mixture of tailings and discards. Demonstration of the efficacy of the procedure was assessed by analyzing effluent solution concentrations of the concurrently operated simulated ore beds following inoculation with micro-organisms implicated in bioleaching (biotic mode) or in the absence of inoculation (abiotic mode). The presence of fine tailings both minimized the infiltration of oxidants to the porous ore and void space within the packed bed and provided neutralisation. In biotic mode, tests with layered covers of desulfurised tailings were less successful at limiting microbial activity and associated accelerated oxidation reactions. Blended columns resulted in reduced leaching reactions and an increase in the mean residence time of the solution phase. By increasing the solution residence time, an aqueous cover was concurrently formed, evolving into a bifunctional mitigating measure

Introduction

Contrary to leaching, ARD mitigation is achieved by inhibiting the oxidation of the sulfide minerals to alleviate the generation of highly toxic acidic runoff, rich in sulphate and deported metals, that may last decades and possibly centuries, requiring prolonged treatment operations and associated costs. Prevention may be achieved by reducing the permeability, and hence the exposed surface area, of the acid-generating waste rock dumps to the elements. Several methods have been proposed that include the use of coatings, covers and cemented paste backfills. Coatings form, often acid-sensitive, films or precipitates that surround the ore surface forming a passivating layer to inhibit the oxidation reactions and subsequently mitigate ARD generation. Alternatively, cemented paste backfills that incorporate sulfide concentrates following desulfurisation by flotation are used to bifunctionally support mined voids and reduce the infiltration of oxygen to the acid-generating tailings [1]. Efficiency as a preventative measure depends on the strength of the backfill that is susceptible to sulfate attack during the curing process [2]. Covers consisting of a barrier of either water to impose diffusional limitations of oxygen to the reactive tailings or oxygen consuming organic materials are common. Recently covers with capillary barrier effects that limit ARD generation by utilising low sulfur, non-acid generating tailings to both inhibit oxygen transport and increase the neutralizing capacity of waste rock dumps are increasingly investigated [1,3].

ARD prevention studies are frequently limited to batch-like experiments that do not account for the long-term resistance of the mitigating procedure to weathering or flow conditions. The influence of acidic environments or the effect of increased oxidation in the presence of iron- and sulfur-oxidising microorganisms that catalyse the leaching reactions at low pH on the efficacy of the preventative measure are also scarce. In this study, experiments are designed to reduce the permeability of acid-generating coal-associated waste rock by the ingression of inert fine benign desulfurised tailings to enhance mass transfer limitations throughout the reaction environment. The efficacy of the method is assessed by analysing the effluent solution concentrations for long-term prevention of ARD.

Experimental setup

Samples

Interburden coal with an average pore volume of 0.035 cm3/g was obtained from the Waterberg Coalfield in South Africa. The desulfurised tailings were generated from the flotation of an ultrafine bituminous waste coal milled to 75% passing 106 μm from Middleburg region, South Africa. The sulfide flotation procedure, outlined in Mbamba et al. [4] was followed to obtain fine tailings with a total sulfur content of less than 0.78%. The acid generating and neutralizing capacity of both the interburden coal and desulfurised tailings were assessed using acid-base accounting tests. The acid neutralizing capacity (ANC), net acid generation (NAG) and acid producing potential (NAPP) of the samples were determined using a refinement of the ANC method proposed by Skousen et al. and procedures outlined by Stewart et al. (NAG, NAPP) [5,6]. The total sulfur of the discards (1.58%) and benign tailings (0.78%) were determined using a LECO sulfur analyser. The interburden (ANC 20.46 kgH2SO4/t, NAPP 27.99 kgH2SO4/t) was characterized as acid forming while the desulfurised tailings non-acid forming (ANC 57.72 kgH2SO4/t, NAPP -33.82 kgH2SO4/t).

Test Columns

Experiments included the concurrent operation of simulated ore beds with in situ neutralization of acid generating interburden coal waste rock with desulfurised tailings. Test columns consisted of PVC columns (H x D = 1.1 x 0.1 m), operated at ambient temperature and packed with a total 3.5 kg of either interburden waste rock (control columns) or a combination of interburden and desulfurised tailings in varying configurations. Co-disposed interburden coal with desulfurised tailings was investigated to minimize the infiltration of oxidants to the porous ore and void space within the bed. Consequently, in tests where the effectiveness of covers was investigated, columns were packed with four alternating layers of interburden with benign tailings. Each layer was composed of 0.625 kg interburden followed by 0.250 kg desulfurised tailings. To further minimize permeable cavities that may be present, columns consisting of a blended mixture of interburden (2.5 kg) and desulfurised tailings (1 kg) were also packed. Due to compactness of packing, test columns were fitted with an overflow to collect any excess irrigant that did not permeate through the bed.

The columns were irrigated from above at 30 mL/h with either water or water acidified with 96 – 98 % concentrated sulfuric acid adjusted to pH 2. These columns were either inoculated with a mixed culture of iron- and sulfur-oxidising mesophilic microorganisms at 1010 cells / ton ore (biotic mode) or uninoculated (abiotic mode). The measured liquor volume, collected at the column outlet, was analysed for pH, redox potential (Ag/AgCl SHE), [Fe2+] and total iron concentration [7]. The latter concentrations, measured spectrophotometrically, provide an indication of the extent of the oxidation reactions and suitability of the mitigating procedure to minimize ARD.

Results and discussion

To establish the most efficient mode of operation, the effect of packing configuration of co-disposed interburden coal with desulfurised tailings on the evolution of leachate pH and redox potential was determined (Fig. 1). We hypothesized that by minimising the infiltration of oxidants to the porous ore and void space within the bed, ARD generation could be minimized or eliminated.

The potential and rate of ARD generation is largely measured by the change in the system pH and the ferric-to-ferrous redox couple (Fig. 1).  On irrigation with water, and to a lesser extent acidified water, the pH rapidly dropped over the first 24 hours.  The initial decrease in pH, and consequently the redox potential, presented in all columns was attributed to the rapid oxidation of fine grain pyritic interburden particles promoting the transport of soluble metals Fe2+ and protons H+ into the aqueous phase. The initial liberation of ferrous ions into the solution phase and the presence of air, subsequently promoted acid consuming oxidation reactions forming ferric ions, increasing both the pH and redox potential. Following the ferric ion oxidation of sulfide minerals there was a net acid generation, and hence ARD potential, with a resulting decrease in pH.

Figure 1. Leachate pH and redox potential for columns containing only interburden coal (control – 100% interburden: a & b), alternating layers of desulfurised tailings with interburden (cover – 60% interburden + 40% desulfurised tailings: c & d) and a blended mixture of interburden with desulfurised tailings (blend – 60% interburden + 40% desulfurised tailings: e and f). In either configuration, the columns were irrigated with either water () or acidified water at pH 2 in either abiotic () or biotic mode ()

In abiotic and biotic mode, the pH of the control column remained near the feed pH 2 after the initial increase over the first 8 days (Fig. 1a). While the redox potential over this period increased to and remained ca. 640 mV (wrt to Ag/AgCl) for the duration of the test (Fig. 1b). On introducing desulfurised tailings as either a layered cover or a blended mix with interburden, the pH and redox potential remained constant over the course of the experiment irrigated with water (Fig. 1 c – f). The alkalinity of the desulfurised tailings in columns fed with water and acidified water at pH 2 successfully neutralised the net acid generation of the leaching reactions maintaining the pH at ca. 7.4 (cover, Fig. 1c) and 7.6 (blend, Fig. 1e). Both column configurations, irrespective of the irrigation feed pH, showed potential to mitigate ARD by limiting the infiltration of oxidants to the sulfide mineral surface. However, the capacity of the layered covers of fine desulfurised tailings to neutralise the sulfide tailings decreased after 68 days for the column operated in biotic mode (Fig. 1 c and d). It is proposed that, prior to this, the microbial activity within the biotic cover test was dormant contributing very little to catalysing oxidation reactions. Thereafter, the microorganisms accelerate the microbial oxidation of ferrous ions in solution promoting an increase in the redox potential (Fig. 1d). The absence of microbial oxidation observed in blended columns are likely due to the tight packing of the mixture of desulfurised tailings and the interburden. Consequently, the void space within the packing was rigorously decreased limiting the oxygen transfer necessary for microbial growth and pyrite oxidation.

The ability to blind the permeable reactive layer of the interburden decreased after 42 days in the abiotic blended column (Fig. 1 e and f). This was indicated by the gradual decrease in pH and redox potential up to ca. 117 days and accelerated thereafter  (Fig. 1 c and d). The exit flow rate increased from 16 mL/h to 22 mL/h during this period resulting in stable pH and redox potentials comparable with those in the control columns (Fig. 1 c and d). Excess feed to the column that did not pass through the ore bed was collected via. the overflow for columns packed with benign tailings. The feed rate remained constant for the test, resulting in preferential flow paths being established early [8]. With time, these paths likely altered culminating into the observed accelerated flows due to reaction and a shift in fines within the ore bed. With increasing solution contact and exposure of the mineral surface to the oxidants, the leaching reactions increased influencing the mitigating efficiency of the blended tailings. This phenomenon was not observed in the remaining columns where mean residence times of liquor remained constant. Here, due to their packing efficiency, the columns were saturated creating an aqueous cover which further enhanced the mitigating efficiency of the desulfurised tailings on ARD generation.

Conclusions

The efficiency of utilizing benign desulfurised tailings packed with acid generating interburden to simultaneously blind the ore surface, minimize weathering and neutralise leaching reactions was studied. By increasing the solution residence time, an aqueous cover was formed evolving into a bifunctional mitigating measure. In biotic mode, there was a significant delay prior to microbial acitivity. Only columns utilising desulfurised tailings as a cover were appreciably affected. Mass transfer limitations imposed by the compactness of blended columns attributed to microbial inactivity enhancing the efficiency of the mitigating procedure. The efficacy of the preventative measure was largely dependent the ability to restrict flow. Columns loaded as alternating layered covers of desulfurised tailings in abiotic operation appeared, in the short-term, to maintain the pH above neutral conditions with the least amount of leaching occurring.

References

[1]	I. Demers, B. Bussière, M. Benzaazoua, M. Mbonimpa, A. Blier: Miner. Eng. (2008) Vol. 21, p. 317.

[2]	M. Benzaazoua, P. Marion, I. Picquet, B. Bussière: Miner. Eng. (2004) Vol. 17, p. 233.

[3]	R.S. Gautama, G.J. Kusuma, I. Lestari, R.P. Anggana: In Proc. 2010 Int. Mine Water Assoc. Symp. Mine Water Innov. Think. (2010).

[4]	C. Mbamba, J.-P. Franzidis, S.T.L. Harrison, J.L. Broadhurst: J. South African Inst. Min. Metall. (2013) Vol. 113, p. 399.

[5]	J. Skousen, J. Renton, H. Brown, P. Evans, B. Leavitt, K. Brady, et al.: J. Environ. Qual. (1997) Vol. 26, p. 673.

[6]	W.A. Stewart, S.D. Miller, R. Smart: In Proc. 7th Int. Conf. Acid Rock Drainage. ICARD (2006) p. 2098.

[7]	R.P. van Hille, A.W. van Zyl, N Spurr and S.T.L. Harrison. Miner. Eng. (2010) Vol. 23, p. 518.

[8]	C.L. Lin, J.D. Miller, C. Garcia: Miner. Eng. (2005) Vol. 18, p. 1045.